Basic Rules for a Successful Application

- The road surface MUST be dry and clean – clear of dust and contaminants

In fact if the road surface is dry and you squeegee out the resin and then broadcast on the aggregate it can then rain as much as it likes.  Even though the resin has not yet cured it will be fine.  BUT it must not rain before the aggregate has sunken into the resin.  Literally only five minutes after the resin has been fully “blinded” (covered) with aggregate it can rain all it likes and it will not make any difference.

- You MUST use a professional "DRILL & PADDLE" to mix the material - not a stick or other manual method.

- You MUST PUSH THE PADDLE ALL THE WAY TO THE BOTTOM OF THE DRUM to ensure the dense (heavy) hardener at the bottom of the drum is thoroughly mixed in with the base material.  Mixing should continue for at least three to five  minutes.  Make sure the paddle goes to the bottom and mixes both part a and b fully - THIS IS CRITICALLY IMPORTANT.

Failure to mix properly will result in DISASTER

- Always mix complete packs.  Do not try to mix part packs

- When applying the resin – you MUST use our squeegees because the serrated teeth are the perfect height to create a 1.0mm to 1.5mm film of resin on the ground.  Please make sure that after spreading  the resin out with our squeegee you WAIT for 5 to 10 minutes BEFORE broadcasting on the aggregate.  This is important because the resin is self levelling and it will take approximately 5 to 10 minutes for the resin to level out so there are no valleys and mountain tops in the resin. This will ensure that a 1-3mm aggregate is embedded by in the resin by 1/3rd or 1mm.

- Make sure you fully blind the resin (cover the resin) with aggregate so you cannot see any resin at all

- Do NOT walk on the aggregate or try to push it down.

- Allow as much time as possible for the resin to cure preferably overnight if possible before opening to traffic.